## Slide 1: SPM in In-CAEM - CAT
Aitor Mugarza
Carmen Ocal

## Slide 2: Infrastructure for Correlative Analysis of Energy Materials
In-CAEM will develop a singular infrastructure for research in advanced energy materials in order to address the scientific challenges of the European Green Deal:
Multi-modal
Multi-lengthscale in situ/operando experiments, combining
Correlative
Open to all the scientific community.
Mix & Match techniques and methodologies to tackle complex problems
Single entry point: ALBA User office
(Scanning) transmission electron microscopy
Scanning probe microscopies
Synchrotron X-rays (spectroscopy, diffraction,…)
Advanced data analytics (HPC, deep learning, AI,…)

## Slide 3: SPM techniques
Atomic
(BR)-STM
Electronic
(STS)
Vibrational
(IETS, Action Specroscopy)
Magnetic
(IETS, Kondo STS, SP-STS)
Atomic manipulation
STM
AFM
Chemical
(F(z))
Magnetic
(MFM)
Electrostatic
(KPFM, SCM, EFM)
Piezoelectric
(PFM)
Friction
(LFM)
Nanolitography
Electrical
(c-AFM)
Notes: -Violin analogy

## Slide 4
UHV 5K STM/nc-AFM
+
photon spectroscopy
Environmental AFM
+
photon spectroscopy
Multipurpose
AFM
UHV STM/nc-AFM
SPM Platform
Ultra-High Vacuum
Environmental, gas/liquid

## Slide 5
UHV 5K STM/nc-AFM
+
photon spectroscopy
Environmental AFM
+
photon spectroscopy
Multipurpose
AFM
UHV STM/nc-AFM
SPM Platform
SPM + Photon spectroscopies
SPM

## Slide 6
UHV 5K STM/nc-AFM
+
photon spectroscopy
Environmental AFM
+
photon spectroscopy
Multipurpose
AFM
UHV STM/nc-AFM
ICN2
Aitor Mugarza
ICMAB
Carmen Ocal
Esther Barrena
SPM Platform
Emigdio Chavez
Roger Palacios
Daniel Martín
Scientist
Laser Technician
SPM Technician
Alba Cazorla

## Slide 7
STM
AFM
XPS/ARPES
MBE
PLD
Globe Box
NAP-XPS
PEEM/LEEM
XAS/XMCD
Magnetic scatt.
ARPES
Mounted on BOREAS beamline
Mounted on glove box
UHV connection of 10 different facilities of ICN2 and ALBA
Connecting Facilities at ICN2-ALBA

## Slide 8
M. G. Cuxart et al. ACS Nano 14, 6285 (2020)
M. Caputo et al., Nano Lett. 16, 3409 (2016)
In-situ:
Materials growth
Atomic scale structural & electronic properties
Band structure
Element-resolved magnetic properties
In-situ multimodal spectroscopy: SPM + synchrotron
@ BOREAS
ICN2-ALBA

## Slide 9
In-situ Multimodal STM + XMCD
Lanthanide-based Metal-organic frameworks
Dy-TPA
STM @ BOREAS
XMCD magnetization curves @ BOREAS
IMDEA-ICN2-ALBA
S. O. Parreiras et al., Small 17, 2102753 (2021)
ICMA-ICMAB-ICN2-ALBA
E. Bartolomé et al., Solid State Phenom. 257, 219 (2016)
E. Bartolomé et al., J. Phys. Chem. C. 124, 13993 (2020)
FePc
FePc + 2O
Oxidation of FePc on Ag(110)

## Slide 10
K. Kuhnke, et al. Chem. Rev. (2017)
Photon SPM
Electroluminiscence
Photoluminiscence
Raman
Photoelectron tunneling

## Slide 11
Scanning tunnelling Luminiscence (STL): 2D materials
Electroluminescence from individual atomic defects
B. Schuler et al., Sci. Adv. 6, eabb5988 (2020)
J. Xu et al., Science 371, 818–822 (2021)
Raman at the single-bond limit

## Slide 12
5) Surface potential / work function (Kelvin Probe Force Microscopy)
3) Current intensity (Conductive AFM)
Correlative AFM
1) Topography
2) Lateral force
(Friction Force Microscopy)
4) I-V spectroscopy
(Conductive AFM)
Correlative topo + multimodal maps of graphene percolated networks synthesized in SiC and Si3N4 composites
ICV-ICMAB
C. Ramírez et al., Carbon 153, 417 (2019)
P. Miranzo et al., J. Eur. Ceram. Soc. 36, 3073 (2016)
C. Ramirez et al., Carbon 49, 3873 (2011)
P. Miranzo et al., J. Eur. Ceram. Soc. 33, 1665 (2013)
Carmen Ocal
Esther Barrena

## Slide 13
Correlative AFM + FESEM + -Raman
Correlative topo + multimodal maps of graphene percolated networks synthesized in SiC and Si3N4 composites
Carmen Ocal
Esther Barrena
ICV-ICMAB
C. Ramírez et al., Carbon 153, 417 (2019)
P. Miranzo et al., J. Eur. Ceram. Soc. 36, 3073 (2016)
C. Ramirez et al., Carbon 49, 3873 (2011)
P. Miranzo et al., J. Eur. Ceram. Soc. 33, 1665 (2013)

## Slide 14
Virwani et al. B. J. Nanotechnol. 2019
In situ AFM imaging of Li-O2 electrochemical reaction on highly oriented pyrolytic graphite with ether-based electrolyte
In situ EC-AFM
Reversible formation of reaction products during the discharge–recharge cycles correlate with the simultaneously recorded electrochemical data.
1M LiNO3 in TEGDME with 2500 ppm of water
3D volume analysis
1M LiNO3 in TEGDME with < 20 ppm of water
In-situ EC-AFM:
- Electrode status
- Deposition dynamics
- Chemical info missing!
Notes: 1.- for 20 ppm: discharge capacity not limited by clogging of the electrode by the deposits, some area still clean. Attribute to O2 depletion due to slow diffusion (high transfer resistance)
2.- AFM gives topography but no chemical identification: other techniques necessary! NAP-XPS, Raman…
The two figures at the bottom demonstrate the reversible “material growth/de-growth” as the product of the physical processes taking place on the cathode surface of a highly reactive lithium–oxygen battery system at different water concentrations in the solvent.
The topographic AFM images taken during the discharge/recharge cycles (at the marked points at black/blue data) capture the formation of discharge products as correlated electrical and topographical channels.
The impact of the presence of water in the solution is measured by varying the water concentration (low concentration at the left and high concentration at the right): there is an increase in the cell discharge capacity at increased water concentration by modifying the charge transfer resistance.
The shape and size of the deposits at different discharge capacity gives information on the kinetics of the processes.
Figure at the top right: The analysis of the volume of precipitates indicates the onset of the process (threshold capacity) and the (second-order polynomial function) behavior of the cell.

## Slide 15
A. Pinilla et al. Carbon 200, 227 (2022)
Raman spectroscopy for H2 generation
In situ detection of the hydrogen generation in electrochemical cell by Raman
Add spatial resolution of
~10-50 nm by TERS
ICN2-IREC-ICFO
Emigdio Chavez

## Slide 16
=
SINGULAR INFRAESTRUCTURE
FOR
ADVANCED MATERIALS
CHARACTERIZATION
Thanks!!
SPM Platform @ ALBA