## Slide 1
Novel Chaclogenide and Chalcohalide Semiconductors for Next Generation Thin Film Solar Cells
By: Kunal J. Tiwari Ph.D.
Post Doctoral Researcher IREC & UPC Barcelona
Kunal J. Tiwari, Dr. Sergio Giraldo, Prof. Zacharie Jehl Li Kao, Prof. Marcel Placidi, Prof. Edgardo Saucedo

## Slide 2
Kunal J. Tiwari Ph.D. Catalonia Institute for Energy Research (IREC) & Polytechnic University of Catalonia (UPC-BarcelonaTech), Barcelona, Spain.
Investigating chalcohalide semiconductors for thin film PV application.
Materials of interest:(Sb/Bi)2Se3 and other emerging binary chalcogenides and chalcohalides.
Research Interest: Exploratory materials synthesis for solar to energy and fuel conversion. Advanced optical characterizations for materials and devices, device simulations(solar cells).
Emerging 2D materials e.g. MXene for application as selective contacts in opto electornic devices.
Interested in learning about:
Development of methods and techniques for advanced optoelectronic characterization of semiconductors.
Interface engineering and study of interface between 2D MXene and Quasi 1-D chalcohalide semiconductors
Research Group
https://www.irec.cat/research/group/solar-energy-materials-and-systems/
http://sensate.eu/
Visit us for more information:

## Slide 3
Active Research Lines
Development of the methods to deposit absorbers with controlled orientation
Exploration of new device structures
Incorporation of halides such as Br, I to realize mix chalcohalide compounds
Synthesis methods such as above ambient pressure reactive thermal annealing.
Interface modification with MXene´s and organic interlayers
Device simulation and development of advanced optoelectronic characterizations tools for materials and device characterization
Sb/Bi Chalcogenide
Sb/Bi Chalcohalide
Charge Selective Contacts
Research Facilities
Materials Processing
Institutional Infrastructure
Characterization

## Slide 4
Background and Important Properties of antimony chalcohalide materials
Sb
Se/S
I/Br
Bi
Ferroelectric
Large dielectric constant
Photoconductive
Suitable Eg and α
Photoferroelectrics
Effect on PCE?
Relatively less explored as compared to other compound semiconductors of this class.
Interesting platform for exploring the exotic properties such as contribution of ferroelectric behavior on photoelectric properties.
Detailed optoelectronic characteristics are not reported till yet.
Prospective applications beyond PV such as PEC, Memristors etc.
Why Chalcohalides??

## Slide 5
SbSeI
I. Caño et al, under preparation.
250ºC
275ºC
300ºC
2 bar
7 bar
14 bar
250ºC / 2 bar
275ºC / 2 bar
300ºC / 2 bar
450ºC / 2 bar
SEM – Formation of SbSeI micro-columnar structures
Increasing T  height and density of micro-columnar structures increases
Thickness and uniformity of unreacted Sb2Se3 layer decreases
450ºC
450ºC
500ºC
Sb2Se3 – 500 nm
SbSeI
Mo
Preliminary Results
Notes: This slide is good

## Slide 6
SbSeI
I. Caño et al, under preparation.
250ºC
275ºC
300ºC
2 bar
7 bar
14 bar
250ºC / 2 bar
275ºC / 2 bar
300ºC / 2 bar
450ºC / 2 bar
450ºC / 7 bar
Sb2Se3
SbSeI
SEM – Formation of SbSeI micro-columnar structures
Increasing T  height and density of micro-columnar structures increases
Thickness and uniformity of unreacted Sb2Se3 layer decreases
Increasing P  height of micro-columns decreases
Tunable morphology by modifying annealing conditions
450ºC
450ºC
500ºC
30 mm
6 mm
10 mm
500ºC / 14 bar
6 mm
Thickness (t) vs. Temperature (1/kT)
Similar Ea for SbSeI formation and Sb2Se3 consumption  process intimately linked
Low Ea  conversion to SbSeI is very favorable process
Preliminary Results
Notes: This slide is good

## Slide 7
SbSeI
I. Caño et al, under preparation.
250ºC / 2 bar
275ºC / 2 bar
300ºC / 2 bar
450ºC / 2 bar
450ºC / 7 bar
500ºC / 14 bar
Sb2Se3
SbSeI
XRD – Detected phases of Sb2Se3 (unreacted layer) and SbSeI
Sb2Se3 amount decreases as T increases
Full conversion to SbSeI at 450ºC – no preferred orientation
Structural and crystallographic characterization
HR-TEM – Performed on a lamella of 450ºC / 2 bar sample
Excellent crystalline quality of micro-column structures
Constituted by a single crystal – absence of grains
Preliminary Results
Notes: This slide is good

## Slide 8
SbSeI
I. Caño et al, under preparation.
Optoelectronic characterization
J-V measurements
External Quantum Efficiency
275ºC | 1.25 eV
300ºC | 1.78 eV
Bandgap:
Sb2Se3
SbSeI
Lower Eg due to Sb2Se3 absorption (layer of unreacted precursor)
300ºC
Voc up to 550 mV (among the highest reported for SbSeI)
Low Jsc & FF  poor carrier collection (columnar morphology)
Bandgap of 1.8 eV – SbSeI is the dominant phase
275ºC
Voc around 550 mV, with PCE close to 1%
Both Sb2Se3 and SbSeI phases absorbing  contribution of a low Eg material (1.25 eV)
Mo/SbSeI/CdS/ZnO/ITO samples
Previous results (solution-based)8
8 YC Choi, K Jung, Nanomaterials, 2021, 11, 3206
275ºC | 21 meV
300ºC | 31 meV
Urbach energy
Preliminary Results
Notes: Discuss also some applications beyond PV maybe?

## Slide 9
SbSeI Conclusion
I. Caño et al, under preparation.
SbSeI micro-columnar samples have been synthesized by high-pressure iodination of Sb2Se3 thin films
  Morphology can be tuned by varying annealing conditions (T and P)
  Samples annealed at T ≤ 300ºC  Sb2Se3 unreacted layer. Its amount decreases with increasing T
  T = 450ºC  Full conversion to SbSeI (no secondary phases)
Proposed formation model: columnar structures are form by a self-catalyzed SLV mechanism (solid-liquid vapor)
  Decomposition of SbI3 to realease I2(g)
  Sb2Se3(s) + I2(g)  2SbSeI(s) + Se(l)
  Precipitation of SbSeI(s) from the liquid-Se leads to formation of micro-columnar morphology
First promising solar cells show Voc values up to 562 mV
  Bandgap = 1.8 eV
  Low Jsc due to poor carrier collection leads to PCE slightly above 0.3%
Sb2Se3
SbSeI
SbI3
NEXT STEPS
Improve front contact
Full coverage by Atomic Layer Deposition (ALD)
New selective contacts: oxides (TiO3, VO5)
Improve carrier collection  Jsc ↑
Expand the family of quasi-1D chalco-halides
SbSeBr
BiSeI
SbSI
Sb(Se,S)I
(Sb,Bi)SeI
…
SbSeI
SbSeBr5
5 KT Butler, JM Frost, A Walsh, Energy & Environmental Science, 2015, 8, 838
New synthesis routes
PVD: Co-evaporation
Solution-based:
SbI3 deposition on Sb2Se3 films
Single-source precursors

## Slide 10
Future Research Directions
Physico-chemical
Band Structure
Intrinsic Carrier Dynamics
Performance Limiting Factors
Carrier Dynamics
Transport layers screening
Absorber
Device
Utilization of advanced characterization methods to develop a more complete understanding of these emerging compound semiconductors

## Slide 11
Thank You
We always remain open for suggestions and collaborations.