REXS2025- International Conference on Resonant Elastic X-ray Scattering

Controlling Skyrmion Lattice Dynamics

with Thermal and Magnetic Field Gradients

H. Jin1, J. Chen1, G. van der Laan2, S. Zhang1, T. Hesjedal2,3

1School of Physical Science and Technology and ShanghaiTech Laboratory for Topological Physics, ShanghaiTech University, Shanghai 201210, China
2Diamond Light Source, Harwell Science and Innovation Campus, Didcot OX11 0DE, UK
3Department of Physics, Clarendon Laboratory, University of Oxford, Oxford OX1 3PU, UK

# ABSTRACT

Magnetic skyrmions exhibit a rich landscape of dynamical behavior shaped by their topological character and collective organization. In this work, we explore the motion of skyrmion lattices in chiral magnets under two orthogonal driving mechanisms: magnetic field gradients [1] and thermal gradients [2,3]. Using resonant elastic x-ray scattering (REXS) on Cu2OSeO3, we demonstrate how finite-sized skyrmion lattices respond to these drives not only by translation, but also by rotation, undergoing a coherent rolling motion driven either by magnon flow (in thermal gradients) [2] or by field-induced torques [1]. The rotational sense and velocity scale predictably with gradient strength and crystallite size, revealing the emergence of a chiral lattice torque, also allowing for the direct measurement of the skyrmion Hall angle in the lattice state [4]. To access the three-dimensional nature of skyrmion textures, we complement these surface-sensitive studies with small-angle neutron scattering (SANS) experiments on MnSi [3]. There, we uncover depth-resolved bending of skyrmion strings under two-dimensional thermal gradients, driven by a temperature-dependent skyrmion Hall effect and governed by a modified Thiele equation incorporating magnon friction. This dual approach, combining high-resolution REXS at the surface and SANS through the bulk, offers a unified view of skyrmion lattice dynamics and demonstrates new modalities for manipulating topological spin textures in three dimensions.

# References

- Shilei Zhang, Weiwei Wang, David M. Burn, H. Peng, Helmuth Berger, Andreas Bauer, Christian Pfleiderer, Gerrit van der Laan, and Thorsten Hesjedal, Manipulation of skyrmion motion by magnetic field gradients, Nature Communications 9, 2115 (2018).

- Haonan Jin, Jingyi Chen, Gerrit van der Laan, Thorsten Hesjedal, Yizhou Liu, and Shilei Zhang, Rolling Motion of Rigid Skyrmion Crystallites Induced by Chiral Lattice Torque, Nano Letters 24, 12226-12232 (2024).

- Kejing Ran, Wancong Tan, Xinyu Sun, Yizhou Liu, Robert M. Dalgliesh, Nina-Juliane Steinke, Gerrit van der Laan, Sean Langridge, Thorsten Hesjedal, and Shilei Zhang, Bending skyrmion strings under two-dimensional thermal gradients, Nature Communications 15, 4860 (2024).

- Richard Brearton, Luke A. Turnbull, J. A. T. Verezhak, Geetha. Balakrishnan, Peter D. Hatton, Gerrit, van der Laan, and Thorsten Hesjedal, Deriving the skyrmion Hall angle from skyrmion lattice dynamics, Nature Communications 12, 2723 (2021).