## Slide 1: Exploring the Electronic and Magnetic Properties of Conventional 2D Materials and 2D MOFs: Insights from Photoelectron Emission Microscopy
🔬 PEEM ➡️ (X)PEEM ➡️ ef-peem ➡️ momentum peem 🔬
Vitaliy Feyer
Peter Grünberg InstitutE PGI-6 “Electronic Properties”
03/2025

## Slide 2: outline
Scientific motivation
Immersion lens microscopy
Chemical selectivity
Energy and Spin filtering

## Slide 3: outline
Scientific motivation
Immersion lens microscopy
Chemical selectivity
Energy and Spin filtering

## Slide 4: Challenge: characterization on the nanoscale
TMO

## Slide 5: PEEM Evolution since 1970
50 years of PEEM: From UV light to synchrotron radiation
UV-PEEM
Balzers Methioskop
  Hg discharge lamp (~5eV)
  surface imaging
  cryst. orient.
  work function
  narrow band exc.
XPEEM
  pol. synchrotron radiation
  elem. selectivity (XAS)
  magn. contrast (XMCD, XMLD)
  electron yield
✚
energy-filtered PEEM
  energy E selection (XPS)
  soft / hard X-rays
  information depth
  time resolution
✚
momentum PEEM
✚
~1970
~1990
~2000
~2015
  easy r - k switching
  momentum k selection (ARPES)
  real/momentum space imaging
  spin P selection

## Slide 6: outline
Scientific motivation
Immersion lens microscopy
Chemical selectivity
Energy and Spin filtering

## Slide 7: Ernst Brüche (1933)
holes in Zn metal plate

## Slide 8: History
Same instrument, 1934!
Polycrystalline Pt foil.
Engel, 1970, group of Ruska
Magnification 2.5x
Magnification 10,000x

## Slide 9: Immersion lens microscope (since 1990)

## Slide 10: momentum microscope
Real space vs. reciprocal space: which image to project on the detector?
• same emission angles: focused in the momentum image plane
• different emission angles from the same spot: focused in the spatial image plane

## Slide 11: Principal imaging modes of an EEM
x
y
real space imaging
reciprocal space imaging
B
A
  lateral distribution of emitted electrons from elements A and B
  angular distribution of photoelectrons
  switch between imaging modes by a single lens
Secondary and photoelectrons
Only photoelectrons

## Slide 12: Synchrotron Light Source
Simple source: Bending magnet
Better source: Wiggler/Undulator
photon energy
flux

## Slide 13: outline
Scientific motivation
Immersion lens microscopy
Chemical selectivity
Energy and Spin filtering

## Slide 14: X-ray Absorption Spectroscopy (XAS)
near-edge
chemistry/magnetism
extended XAFS
atomic structure
incident beam
transmitted beam
inelastic scattering, fluorescence
total/partial electron yield
A
drain current
Experimentally there are different ways to do XAS:
Typical XAS spectrum
relevant to PEEM!

## Slide 15: LSMO resistive switching (ex-situ)
RS in ferromagnetic La0,7Sr0,3MnO3(LSMO)
☞ M. Wilhelm, at al., APL Materials 8, 111102 (2020)
  ReRAM (Resistive Random-Access Memory) is a type of non-volatile memory that stores data by changing the resistance of a material.
  It relies on the formation and dissolution of conductive filaments within an insulating layer when an electrical voltage is applied.

## Slide 16: LSMO resistive switching (ex-situ)
RS in ferromagnetic La0,7Sr0,3MnO3(LSMO)
☞ M. Wilhelm, at al., APL Materials 8, 111102 (2020)
  ex-situ switching at different voltages
  4 - 5V HRS state changes in region
  clear spectral signature of resistive switching Mn3+/4+ ⟹ Mn2+/3+
  close link to magnetism (XMCD signature)

## Slide 17: outline
Scientific motivation
Immersion lens microscopy
Chemical selectivity
Energy and Spin filtering

## Slide 18: x-ray photoemission spectroscopy (XPS)
vs the kinetic energy of the emitted electron
photon
Binding
energy
Kinetic
energy
hν ≈ B.E. + K.E.
Need to determine the kinetic energy of photoelectrons
(kinetic energy) = hν – (work function) – (binding energy)

## Slide 19
Typical XPS spectrum
(kinetic energy) = hν – (work function) – (binding energy)
X-ray Photoemission Spectroscopy (XPS)

## Slide 20
Valence electron photoemision
Periodic potential  electronic bands
and band gaps

## Slide 21: energy-filtered microscopes
US=–20 kV US=–20 kV US=0

## Slide 22: Spin filtered momentum microscope
  Spin filtering by reflection at W(100) mirror
  Alternative spin filter Au/Ir(001)
  Simultaneous detection of 104 data points!
FoM2D =37@11.50eV
D. Vasilyev, C. Tusche, F. Giebels, H. Gollisch, R. Feder, J. Kirschner: J., Electron Spectrosc. Relat. Phenom. 199, p10-18 (2015)

## Slide 23: 2D Materials: NiTe2 layered semimetal

## Slide 24
ENERGY- AND Spin-Resolved momentum space

## Slide 25: k-space imaging mode: momentum microscopy

## Slide 26: Type-II dirac semimetal
NiTe2: Fermi surface tomography
  Various cuts through the Fermi surface
  dispersion maps at different photon energy
  bulk bands (blue)

## Slide 27: Spin texture of the surface Dirac cone
Above the surface Dirac point:
Characteristic spin-momentum locking is observed.
Below the surface Dirac point:
Reversed spin polarization emerges.

## Slide 28: Spin texture of the bulk Dirac cone
Hidden spin polarization originates from broken inversion symmetry at the surface Te layer.
Observed Py spin texture is anti-symmetric with respect to kₓ = 0, consistent with mirror symmetry

## Slide 29: graphene

## Slide 30: Growth method (CVD) and substrate
CVD
exfoliation
Chemical Vapor Deposition
catalytic decomposition of hydrocarbons (methane, ethylene, propane, acetylene, …)
accumulation of C on the surface
substrate with hexagonal symmetry
lattice constant similar to the graphene one (only 1.8 % mismatch)
easy magnetization axis

## Slide 31: Effect of the substrate
Graphene on weakly
interacting substrates
C. Riedl et al., J. of Phys. D 43 (2010) 37
EF
Free-standing graphene
Graphene on strongly
interacting substrates
Gr/Ni(111)
Gr/Fe(110)
Gr/Co(0001)
Notes: Non interacting substrates  more interacting  magnetic next slide

## Slide 32: Spin-polarized feature in graphene
Dirac-like features close to the Fermi level of Gr/Co/W(110) hybrid are spin polarized
M
Intensity (arb. units)
Spin-integrated
Spin-resolved

## Slide 33: Eu doping of the Gr/Co interface
Eu (1/3 ML) is ordered on top of graphene
Drastic change in the Fermi surface
Graphene is doped
Umklapp leads to band folding
M. Jugovac et al., Advanced Materials (2023) 2301441.
Gr/Co
Eu/Gr/Co
Gr/Co
Eu/Gr/Co

## Slide 34: Eu doping of the Gr/Co interface – spin
M. Jugovac et al., Advanced Materials (2023) 2301441.
Gr/Co

## Slide 35: Eu intercalation at the Gr/Co interface
Eu (1/3 ML) is ordered upon intercalation
Drastic change in the Fermi surface
Graphene is doped
Bandgap at the Dirac point
M. Jugovac et al., Advanced Materials (2023) 2301441.
Gr/Co
Gr/Eu/Co
Gr/Co
Gr/Eu/Co

## Slide 36: Eu intercalation at the Gr/Co interface - spin
M. Jugovac et al., Advanced Materials (2023) 2301441.
Single-spin polarized flat bands at the Fermi level!

## Slide 37: Conclusions
…in Gr/Co(0001)
Eu deposition dopes the electronic bands of graphene
Eu intercalation decouples graphene and dopes it
formation of single spin flat bands at the Fermi level!

## Slide 38: Metal-organic frameworks (2D-MOF)
DOI: 10.1021/acs.accounts.5b00172
Acc. Chem. Res. 2015, 48, 2132−2139

## Slide 39: Experimental techniques
J. Stöhr, Springer Tracts in Modern Physics, 2023, 288
Near edge X-ray absorption fine structure (NEXAFS)
Molecular geometry
Electronic structure
Oxidation state
X-ray magnetic circular dichroism (XMCD)
Electronic and magnetic properties
Spin and oxidation states
Molecular geometry
Photoemission tomography (PT)
Electronic structure, energy level alignment
Charge transfer
Chemical modification
Band structure
3D tomographic imaging of MOs
P. Puschnig et al., Science, 2009, 326,702-706

## Slide 40: Ni-(TCNQ)x
Ni1(TCNQ)1 HC MOF
Ni1(TCNQ)2
LC MOF
By tuning the surface concentration of Ni atoms, we achieve precise control over the formation of two distinct stoichiometric Ni:TCNQ phases.
Stable Ni(I) (d⁹) configuration observed in both 1:1 and 1:2 Ni-TCNQ phases.
Ni→TCNQ charge transfer fills ligand LUMO; extra charge comes from the Ag(100) substrate.

## Slide 41: coordination bonding
Energy level alignment is determined by analyzing the symmetry of ligand orbitals and their interaction with Ni d-states in a square planar field.
Covalent bonding revealed via orbital splitting into bonding/antibonding states.

## Slide 42: Band structure of 2d ni-tcnq mofs
Hybrid bands show clear energy dispersion, proving extended 2D MOF formation.

## Slide 43: Superexchange Coupling in Ni-Based MOFs
XMCD shows only Ni(I) is stabilized on Ag(100) and Au(111), due to strong MOF–metal interactions.
On Ag(100), a planar geometry leads to weak exchange coupling (J = 1.2 meV).
On Au(111), stronger coupling (J = 3.2 meV) arises from altered charge transfer and Ni displacement.
Ni+, S=1/2 state
x2-y2
z2

## Slide 44: an “All-In-One” Photoemission Experiment
Future Evolution
  From UV-PEEM to HAXPEEM
  From Statics to Dynamics
  Without / With Spin

## Slide 45
Interaction of x-rays with matter: useful resources
https://srdata.nist.gov/xps/main_search_menu.aspx
https://vuo.elettra.trieste.it/services/elements/WebElements.html
https://xdb.lbl.gov/

## Slide 46: Spin-Resolved momentum space
  Spin-resolved Fermi surface of Cobalt
C. Tusche, M. Ellguth, V. Feyer, A. Krasyuk, C. Wiemann, J. Henk, C. M. Schneider, and J. Kirschner, Nat. Comm. 9, 3727 (2018).