## Slide 1
Precise Node Metalation in a Zirconium Metal-Organic Framework Enables Highly Efficient PFOA Capture via Synergistic Adsorption Sites
Edouardos Loukopoulos
Institute of Catalysis and Petrochemistry, Spanish National Research Council (ICP-CSIC)
VII ALBA Users’ Meeting, 04/09/2026

## Slide 2
Local-/long-range structural analysis in inorganic materials
Identification of structure-property correlations
Synthetic tailoring for optimized sustainability function
X-ray Absorption Spectroscopy
Pair Distribution Function analysis
2
Synchrotron Characterization to Elucidate Structural Features and Modifications
Chem. Soc. Rev. 2024, 53, 24, 11772
César Nombela - Atracción de Talento Fellow (2026)
Multiscale Characterization in Catalysis group
(LOCAL-MATER)

## Slide 3
Prototypical porous materials: Metal-Organic Frameworks (MOFs)
+
+
Diverse porosity features
High stability
Potential for chemical tailoring
Inorganic
Node
Inorganic
Node
Organic
Linker
Organic
Linker
Saturated, 12-c cluster
Most Zr6-based MOFs
(e.g. UiO-66)
Unsaturated, 8-c and 6-c clusters
(e.g. MOF-808, NU-1000, PCN-222)
Zr6O8 cluster node

## Slide 4
The problem: Increasing decline in water quality, further aggravated by new, man-made pollutants with high persistence and toxicity.
Per-/poly-fluoroalkyl substances (PFAS)
UN 2030 Agenda for
Sustainable Development
Found extensively in everyday applications
Highly toxic for humans and aquatic organisms
Extremely resistant to common water treatments
Limitations of existing PFOA
adsorption-based methods:
Low capacities
Slow kinetics
Low regeneration performance
Perfluorooctanoic acid (PFOA)
Engineering MOF-based systems for Water Decontamination
Solution: Use chemistry-inspired modifications in MOFs to develop target-based sorbents for optimal removal of PFAS from water.

## Slide 5
UN 2030 Agenda for
Sustainable Development
Engineering MOF-based systems for Water Decontamination
Solution: Use chemistry-inspired modifications in MOFs to develop target-based sorbents for optimal removal of PFAS from water.
Parameters to exploit during MOF design / functionalization:
M – OPFAS coordination
H-bonding
Electrostatic forces
Hydrophobic/F-F interactions
Tuning of pore features
(size, hydrophobicity)

## Slide 6
Zr
C
O
Engineering MOF-based systems for Water Decontamination
High air, water and chemical stability
Large pore size (18 Å)
Based on highly unsaturated 6-connected Zr6O8 clusters
Grafting metal sites to enhance PFAS adsorption via coordination binding – The example of MOF-808

## Slide 7
Zr
C
O
Engineering MOF-based systems for Water Decontamination
Binding sites for functionalization
High air, water and chemical stability
Large pore size (18 Å)
Based on highly unsaturated 6-connected Zr6O8 clusters
Grafting metal sites to enhance PFAS adsorption via coordination binding – The example of MOF-808

## Slide 8
Zr
C
O
Engineering MOF-based systems for Water Decontamination
Binding sites for functionalization
Fe-MOF-808
Engineering of iron/acetate binuclear species
Grafting metal sites to enhance PFAS adsorption via coordination binding – The example of MOF-808
J. Am. Chem. Soc. 2026, 148,19, 19672

## Slide 9
Characterization of Fe-MOF-808
Zr
O
Fe
J. Am. Chem. Soc. 2026, 148,19, 19672

## Slide 10
Elucidating the local structure in Fe-MOF-808
Pair Distribution Function Analysis
Fe K-edge X-Ray Absorption Spectroscopy
DFT model

## Slide 11
PFOA adsorption performance
Fast PFOA adsorption kinetics (C = 100 ppm)
PFOA adsorption capacity at C = 1000 ppm
S. Marugán-Benito (ICP-CSIC)
Prof. L. Ahrens (SLU, Uppsala)
t1
C0
C1
Fe sites enhance PFOA removal (C = 100 ppm)

## Slide 12
Post-Capture Characterization
While the main structure remains intact, some PFOA remains strongly-bound after capture

## Slide 13
Synchrotron-based mechanistic investigations
PDF and dPDF analysis suggest formation of coordination binding and weak PFOA∙∙∙MOF interactions

## Slide 14
flow entrance
flow exit
J. Am. Chem. Soc. 2026, 148,19, 19672
Monitoring the Fe environment through in situ XAS
ALBA BL16 – NOTOS:
C. Marini
J. Prat Albert

## Slide 15
J. Am. Chem. Soc. 2026, 148,19, 19672
Monitoring the Fe environment through in situ XAS
C. Marini
J. Prat Albert
S. Marugán-Benito
M. Roselló-González
Progressive exchange of coordinated acetates with PFOA alters absorption intensity with no changes in Fe oxidation state

## Slide 16
J. Am. Chem. Soc. 2026, 148,19, 19672
Monitoring the Fe environment through in situ XAS
C. Marini
J. Prat Albert
S. Marugán-Benito
M. Roselló-González
Coordination of PFOA initially expands the Fe octahedron before eventual stabilization

## Slide 17
Computational Investigations
Theoretical calculations and modelling determine binding site preference
1st PFOA
binds to Zr
-89.3 kJ/mol
Fe-MOF-808
-189.9 kJ/mol
-210.2 kJ/mol
2nd PFOA
binds to Zr
3rd PFOA
binds to Fe
J. Am. Chem. Soc. 2026, 148,19, 19672
A. Mavrantonakis (ICMM-CSIC)
M. Vlachos (ICMM-CSIC)

## Slide 18
Take-home Messages
Node engineering of MOF-808 with secondary Fe centres creates synergistic Zr/Fe binding sites, enabling efficient and rapid PFOA capture.
Binding is further stabilized via electrostatic and hydrophobic interactions.
Synchrotron techniques are essential to determine the local structural environment and extract mechanistic information.
Scan here for the full paper:

## Slide 19
LOCAL-MATER members:
Dr. Ana Platero-Prats
Dr. Rodrigo Gil San Millán
Sergio Marugán-Benito
Miguel Roselló González
Michalis Vlachos
Sofía Barragan Soto
Synchrotron Facilities:
ALBA Synchrotron, BL-16 NOTOS (XAS studies)
Diamond Light Source (PDF studies)
ESRF (PDF studies)
Theoretical calculations:
Dr. Andreas Mavrandonakis (ICMM – CSIC)
Acknowledgments
PFAS adsorption studies:
Lutz Ahrens (SLU, Uppsala)
2025-T1/ECO-36154
Funded
by the European Union