## Slide 1
1
Assessment of thin film superconductivity with
atomic-resolution TEM imaging and analysis in
advanced and innovative materials or heterostructures
Gemma Rius
Institute of Microelectronics of Barcelona, IMB-CNM-CSIC
gemma.rius@csic.es
Superconducting & Hybrid Quantum Chips Research Line qchip.csic.es

## Slide 2
2
Integrated Clean Room for Micro/Nanotechnologies
www.imb-cnm.csic.es/en/sala-blanca-de-micro-y-nanofabricacion

## Slide 3
3
Baseline Superconducting Devices.
Design, Fabrication and Testing
Hybrid Devices and Unconventional Systems
Baseline Supercond. Thin films & Devices
Material | Tc
Aluminum | 1.2
Tantalum | 4.2-4.4
Niobium |  4.5
α-Tungsten | < 100mK
Customized or Advanced
Superconducting Thin films
Nitridized Aluminum
Ultrathin Amorphous WSix
Microwave Resonators, e.g. Al and Ta
Micro – Nano Technologies for Quantum Materials and Devices gemma.rius@csic.es
Manuscript in Prep.
2 Manuscripts under Rev / in Prep.
Paper on Ta-Nb to be submitted
2025 Supercond. Sci. Technol. 38 095004
2024 Supercond. Sci. Technol. 37 035017
Quantum Materials Integration
Semiconductor-Superconductor
2026 J Low Temp Phys 222, 55 doi.org/10.1007/s10909-026-03390-y
2026 IEEE Trans. Appl. Superconductivity 36, 5, 1-5 doi.org/10.1109/TASC.2026.3673788
Superconducting & Hybrid Quantum Chips Research Line qchip.csic.es

## Slide 4
Conventional Methods:
Sputtering
Evaporation
Micro and Nano Patterning
4
Superconducting & Hybrid Quantum Chips Research Line
Material | Tc
Aluminum | 1.2 K
Tantalum | 4.2-4.4 K
Niobium |  4.5-6 K
α-Tungsten | < 100mK
Titanium | 400 mK
Proximitized films | Tunable
Multilayer stacks | Tunable
Paper to be submitted on Nb/Ta Thin films
2025 Supercond. Sci. Technol. 38 095004
Baseline Superconducting
Thin Films and Devices.
Intended for both cryogenic electronics and quantum devices
Design fabrication and testing of DC and MW devices & circuits
Resilience of materials and devices to operation, such as B
Micro – Nano Technologies for Quantum Materials and Devices gemma.rius@csic.es
Qualifying existing (metal) thin films
Developing deposition conditions
Fabrication of devices – based on available equipment
and target materials at the ICTS IMB-Clean Roo
Design, Fabrication and Testing

## Slide 5
Baseline Superconducting Devices.
Design, Fabrication and Testing
Microwave Resonators, e.g. Al and Ta
Designs of circuits, including arrays of multiplexed resonators
Fabrication of devices and external interfacing (pcbs and sample box)
Analysis of performances upon testing in dilution fridge
(cryo-characterization not on-site)
Modelling and simulations for device and
chip design and performance evaluation:
    Sonnet
    COMSOL
Parametric comprehension of actual characteristics and performances: freq, Ql, power, T, SPR…
Optimization by layout design and fabrication processing
Diagnostic and mitigation of effects and sensitivity or resilience
to environment /off-chip experimental conditions, e.g. ionizing radiation
MINARE Project
LSC-LNGS / IFAE / IMB-CNM
APL Quantum 3, 020901 (2026)
doi.org/10.1063/5.0319835
Micro – Nano Technologies for Quantum Materials and Devices gemma.rius@csic.es
Superconducting & Hybrid Quantum Chips Research Line

## Slide 6
6
Baseline Superconducting Devices.
Design, Fabrication and Testing
Microwave Resonators, e.g. Al on Sapphire
Micro – Nano Technologies for Quantum Materials and Devices gemma.rius@csic.es
Superconducting & Hybrid Quantum Chips Research Line

## Slide 7
7
Baseline Superconducting Devices.
Design, Fabrication and Testing
Arrays of CPW Microwave Resonators, e.g. Al on Sapphire
Micro – Nano Technologies for Quantum Materials and Devices gemma.rius@csic.es
Superconducting & Hybrid Quantum Chips Research Line

## Slide 8
8
Baseline Superconducting Devices.
Design, Fabrication and Testing
Arrays of CPW Microwave Resonators
e.g. Al on SiC
Micro – Nano Technologies for Quantum Materials and Devices gemma.rius@csic.es
Superconducting & Hybrid Quantum Chips Research Line

## Slide 9
9
Baseline Superconducting Devices.
Design, Fabrication and Testing
Microwave Resonator Technology - Pure Metals vs Stacks of Thin films.
Ex. substrate/Ti/Al
Enginnering or Advanced Superconducting Thin Films
+
Micro – Nano Technologies for Quantum Materials and Devices gemma.rius@csic.es
Superconducting & Hybrid Quantum Chips Research Line

## Slide 10
10
Microwave Superconducting Resonator Technology, single metals vs Stacks of Thin films. Ex. substrate/Ti/Al
Micro – Nano Technologies for Quantum Materials and Devices gemma.rius@csic.es
Superconducting & Hybrid Quantum Chips Research Line

## Slide 11
11
Microwave Resonator Technology, single metals vs Stacks of Thin films. Ex. substrate/Ti/Al
Micro – Nano Technologies for Quantum Materials and Devices gemma.rius@csic.es
Superconducting & Hybrid Quantum Chips Research Line

## Slide 12
12
Customized or Advanced
Superconducting Thin films
Nitridized Aluminum
Design of tuned or novel superconductivity features
Developing methods and deposition conditions
Fabrication, morphostructural characterization
and functional/operational testing
Tools and Methods:
Sputtering & Evaporation
Ion irradiation (conventional implantation or FIB)
Micro and Nano Patterning of devices
SRIM/TRIM, Tridyn, …
Quantum sensing applications, e.g. direct DM detection
Realization of (ultra) thin films and devices or circuits with specifics in Tc, Lk
Functional/application-oriented design of materials and devices
Ultrathin Amorphous WSix
2026 J Low Temp Phys 222, 55 doi.org/10.1007/s10909-026-03390-y
2024 Supercond. Sci. Technol. 37 035017
2026 IEEE TA Superconductivity 36, 5, 1-5 doi.org/10.1109/TASC.2026.3673788
Micro – Nano Technologies for Quantum Materials and Devices gemma.rius@csic.es
Superconducting & Hybrid Quantum Chips Research Line

## Slide 13
13
Customized or Advanced Superconducting Thin films
Nitridized Aluminum
2024 Supercond. Sci. Technol. 37 035017
2026 J Low Temp Phys 222, 55 doi.org/10.1007/s10909-026-03390-y
Micro – Nano Technologies for Quantum Materials and Devices gemma.rius@csic.es
Superconducting & Hybrid Quantum Chips Research Line

## Slide 14
14
Micro – Nano Technologies for Quantum Materials and Devices gemma.rius@csic.es
Superconducting & Hybrid Quantum Chips Research Line

## Slide 15
15
Advanced Superconducting Thin films. Nitridized Aluminum by Reactive Sputtering
Micro – Nano Technologies for Quantum Materials and Devices gemma.rius@csic.es
Property | Sample 3 - lower N% | Sample 6 - higher N% | Difference
Structure | Nanocrystalline/ polycrystalline | Nanocrystalline/ polycrystalline | Same basic class
Characteristic domain size | ~15–25 nm | ~5–12 nm | Smaller
Average representative size | ~20 nm | ~8–10 nm | ~ 2× smaller
Large coherent regions | Relatively common | Less common | Reduced
Grain-boundary density | Moderate/high | High | Increased
Local lattice coherence | Higher | Lower | More disorder
Local orientation variation | Moderate | High | Increased
Internal lattice distortion | Moderate | Moderate–high+ | Increased
Texture | Somewhat more coherent | More isotropic/mixed | More random
Long-range crystalline order | Limited | Very limited | Further reduced
Sample 3
Al0.9N0.1
Sample 6
Al0.75N0.25
2024 Supercond. Sci. Technol. 37 035017
Superconducting & Hybrid Quantum Chips Research Line

## Slide 16
16
QUTE Project Ref. CNS2023-145234
Ion Irradiation for Advanced Control of Superconductivity in Thin Films
2023 Appl. Phys. Rev. 10, 041311
https://doi.org/10.1063/5.0162597
Micro – Nano Technologies for Quantum Materials and Devices gemma.rius@csic.es

## Slide 17
17
QUTE Project Ref. CNS2023-145234
Ion Irradiation for Advanced Control of Superconductivity in Thin Films
Micro – Nano Technologies for Quantum Materials and Devices gemma.rius@csic.es

## Slide 18
18
Application of Ion-based SC Thin Films - TES
Ultra thin W Tc Tuning via Ion irradiation with semiconductor ions - Si and Ge
Ion Irradiation for Advanced Control of Superconductivity
2026 IEEE Trans. Appl. Superconductivity 36, 5, 1-5 doi.org/10.1109/TASC.2026.3673788
Micro – Nano Technologies for Quantum Materials and Devices gemma.rius@csic.es

## Slide 19
19
Customized or Advanced Superconducting Thin films
Ion Irradiation for Thin Film Tuning AlNx
Micro – Nano Technologies for Quantum Materials and Devices gemma.rius@csic.es
Superconducting & Hybrid Quantum Chips Research Line
2.5 K @ 7.5E16

## Slide 20
20
Manuscript in Prep.
Hybrid Devices and Unconventional Systems
Semiconductor-Superconductor
Magnetic-Superconductor
Innovative developments of fabrication technology/sequences
Realization of quantum grade interfaces and hybrid integration
Fabrication, morphostructural characterization and functional testing
Methodologies:
Shadow Wall patterning, e.g. single step EBL
Epitaxial NWs, selective materials growth, local patterning, mix and match
Coordinated processing and characterization in multiple sites
Assessment and demonstrators of compatible fabrication sequences and device operation
Realization of (ultra) thin films and devices or circuits with specifics in Tc, Lk
Oriented to quantum physics studies and novel quantum computing/sensing applications
Unconventional Approaches and Research on Quantum Technologies
https://doi.org/10.3390/biomimetics10080516
HyFab and IKUR Projects
I-QUMA Project
Micro – Nano Technologies for Quantum Materials and Devices gemma.rius@csic.es

## Slide 21
21
Assessment of Thin Film Superconductivity with
Atomic-resolution TEM Imaging and Analysis in
Advanced and Innovative Materials or Heterostructures
Superconducting & Hybrid Quantum Chips Research Line qchip.csic.es
Atomic/Nano Scale: crystal phase, mono/poly, disorder, amorphization…
Microscopic Morphology: domain size, grain boundaries, texture…
Elemental Composition: purity, doping, stoichiometry, gradients…
Interfacial Analyses: native oxides, epitaxy, intermixing…
Correlative Evaluation: multi-variable properties/characteristics/functionality
SUMMARY

## Slide 22
Thank you
CONTACT: Dr. Gemma Rius gemma.rius@csic.es
Acknowledge ALBA access to METCAM in 2026-I
ALBA METCAM Team
Bernat, Kapil, Belen, Francisco …
Qchip Team at IMB and students
María, Carlo and previous members and students
Nanolitho Area IMB-ICTS Team
Liber, Xevi, Albert…
Clean Room Staff
Leyre, Javi, Nuria, Alberto…

## Slide 23
Thank you
CONTACT: Dr. Gemma Rius gemma.rius@csic.es
Funding Acknowledgements:
QTP2021-03-014; PID2021-122140NB-C32;
TED2021-130292B-C44; CNS2023-145234;
IKUR2025-QT11; Trigger KICKIN; I-QUMA (PID2025)
Main Collaborators and Support:
INRiM, LNGS, CERN, FBK, HZDR, INL
INMA, UAM, CFM-EHU, UV, IFCA-DCOM, ALBA-CELLS, LSC
kiutra, TESCAN