## Slide 1: Surface Science Experiments under Ambient Conditions at ALBA Synchrotron
Juan Jesús Velasco Vélez

## Slide 2: Gaps in material science
R. Schlögl, Angew. Chem. Int. Ed. 2015, 54, 2–58
Structural complexity
and chemical composition
R. Schlögl, Angew. Chem. Int. Ed. 2015, 54, 2–58

## Slide 3
Photoelectron spectroscopy
Kai Siegbahn

## Slide 4: NAP-XPS
HiPP-3 NAP analyzer
PHOIBOS 150 NAP analyzer
Kai Siegbahn
Miquel Salmeron

## Slide 5: NAP-XPS

## Slide 6: Soft NAP-XPS (CIRCE-NAPP)
*Dr. Ravi Ranjan

## Slide 7: Selective hydrogenation Reactions on RAW Pd catalysts
CnH2n-2 (gas)
CnH2n (gas)
CnH2n+2 (gas)
Partial selective hydrogenation
Full unselective
hydrogenation
CnH2n-2 (gas)
Low pressures
High pressures
Pd
Pd

## Slide 8: Alkynes hydrogenation (few mbars)
D. Teschner et al. Science 2008, 320(5872), 86-89.
D. Teschner et al. J. of Cat. 2006, 242(1), 26-37.
~1 mbar!
Surface Pd-C phase blocks diffusion of H to the surface
PdHx
Pd-C
ChemPhysChem 2019, 20, 1158– 1176

## Slide 9: operando NEXAFS - Hydrogenation
with SiNx membrane
Pd @ SiNx membrane; #34305
Hydride peak shape: Tew et al. J. Catal. 283 (2011) 45-54.

## Slide 10: operando NEXAFS - Reaction
Pd @ SiNx membrane; #34305
RT; H2 : C2H2 = 5 : 1
Pressure not enough to investigate the selective/unselective hydrogenation reaction of alkynes to alkenes/alkanes

## Slide 11: Higher working pressures
Electron scattering in gas phase
X-ray
e-
APXPS
Nozzle
D
d
Reducing
surface
and chemical
sensitivity
Ionisation cross section:
J.J. Yeh and I. Lindau, Atomic Data Nucl. Tables 32 (1985) 1.
Inelastic mean free path:
S. Tanuma, J. Powell, D.R. Penn, Surf. Interf. Anal. 21 (1993) 165.
Ionisation cross section
IMFP

## Slide 12: 3Sbar: New beamline for surface characterization
BL15
Surface sensitivity
Total external reflection: X-ray depth control
Signal enhancement!
αi<αc
Evanescent regime
BL15 (3Sbar):
Endstation
Construction finish during 2026
X-ray beam
3SBar will combine ambient pressure X-ray Photoemission Spectroscopy (AP-XPS) at high pressures(1 bar or more) and surface X-ray diffraction (SXRD) and grazing incidence scattering (GISX) angles (-3° to +15°). First beamline optimized for operate in ALBA II.
e–
Gas flow
X-Ray

## Slide 13: Beamline layout
VCM
DiagOn
DCM
Shutter
Slits
Diag1
Diag2
KB
Chopper
Endstation
Attern.
Detector table
GISAXS detec. detector
Parameter | Value | Remark
Energy range | 2.0 keV up to 17.0 keV | 
Flux at 5 keV | 1.76x1013 ph/s | Si(311)
Resolution at 5 keV | 128 meV | Si(311)
Spot size on sample | 1.27 x 3.66 µm2 FWHM | ALBA II
Divergence on Sample | 0.76 x 0.30 mrad2 FWHM | ALBA II
*Josep Nicolas

## Slide 14: 3Sbar detectors and gas environment
Endstation
AEOLOS 150 AD-CMOS
PILATUS4 2M (Si)
Fully automatized gas delivery system:
Two full set of MFCs (ml/min and l/min)
Gases:
He, Ar, N2
H2
O2
CO2
CO
NH3
NxO
CxHy
Vapours:
H2O
Et-OH; Met-OH; etc...
Online gas product analysis:
Gas Chromatography:
SHIMADZU GC-2030N BASIC
2 x QMS:
Edwards WRA200S
Electrochemistry:
Potentiostat:
Biologic SP-300 (2 channels EIS)
Lambda 750 (Si)
Detector table
Gas system

## Slide 15
At the sample stage
Laser heater up to 1200 C
Gas delivery system mass flow controllers from low to high pressure (8 bars)
Mass spectrometry
Gas chromatography
Vapor dosing
Sample preparation
Sputtering
Annealing up to 1400 C
Plasma treatment
PVD
Possible transfer suitcase
Omicron plate (adaptable sample holder)
Multiple thermocouples
Gas dosing (possible flow reactor)
6 pins free to use
*Christopher Goodwin
*Nahikari Gonzalez
*Antoni Garcia
*Christopher Goodwin

## Slide 16: Case study: CO hydrogenation over Fe(110)
Iron is known to make long-chain hydrocarbons
Long chains deactivate the surface
Surface XRD and HP-XPS were performed independently to understand the process
ACS Catal. 2022, 12, 13, 7609
e–
Gas flow
X-Ray

## Slide 17: Incomplete information
By XPS, we know there are two ‘types’ of carbide (Octahedral and trigonal-prismatic)
There are many structures that have these ‘types’ of carbide
O-carbide
TP-carbide
1:4 CO:H2, 85 mbar
ACS Catal. 2022, 12, 13, 7609

## Slide 18
SXRD suggests the only surface structure is θ-Fe3C
SXRD will only detect crystal phases
O-carbide may not be crystalline
ACS Catal. 2022, 12, 13, 7609
SXRD
1:4 CO:H2, 350C, 150 mbar
1:4 CO:H2, 550 mbar
1:4 CO:H2, 85 mbar

## Slide 19
Electrochemical set up
*Andrea Sartori

## Slide 20
Manipulator modified
Sample modification to allow grazing incidence scattering
beam path
Dome like shape to allow grazing incidence diffraction
Elongated shape to get as much signal as possible
*Andrea Sartori

## Slide 21
HER-BiLG/5 nm Pd/FKD (100 mM H2SO4)

## Slide 22
3SBar
Starting with light 6th of November 2026
Endstation/Exp. Environment
Source/Optics/Diagnostics
Users first half 2027 (June/July)
In construction
(finish end 2026/begining 2027)

## Slide 23: Thanks!
3SBar team:
Juan J. Velasco
Christopher Goodwin
Andrea Sartori
WP1(Optics design): Josep Nicolas
WP2 (ID): Jordi Marcos
WP3 (FE): Raquel Monge
WP4 (Optics mechanics): Alejandro Crisol
WP5 (Vacuum): Carles Colldelram/Lizet Carvajal
WP6 (Endstation): Juan J. Velasco
WP7 (Electronics hardware): Albert Miret
WP8 (Electronics infrastructure): Albert Ruz
WP9 (IT system): Adara Carrión
WP10 (Controls): Jordi Aguilar
WP11 (PLCs+PSS): Nil Serra/Jorge Villanueva
WP12 (Radiation shielding): Cristina Orozco
WP13 (Services+control hutch): Núria Martí
WP14 (Cryocooler): Carles Colldelram
WP15 (CNS permit): María José Garcia
WP16 (Gases): Christopher Goodwin
Management :
Caterina Biscari
Josep Nicolás
Klaus Attenkofer
François Fauth
Safety :
Victor Garrido
Josep Maria Roca
Manel Pérez
Carolina Gutiérrez
Administration:
Enric Vinyals
Vanesa Faro
Elisenda Sanchis
Ivette Borrás
Clara Reyero
Edgar Eigner
Juan
Velasco
Chris
Goodwin
Andrea
Sartori

## Slide 24: ALBA vs. ALBA II
Parameter | ALBA (Current) | ALBA II (Upgrade)
Generation | 3rd-generation synchrotron | 4th-generation synchrotron
Electron Energy | 3.0 GeV | 3.0 GeV (same)
Circumference | 268.8 m | 268.8 m (same)
Beam Current | ~250 mA | ~300 mA
Horizontal Emittance | ~4.3 nm·rad | ~0.14–0.2 nm·rad (≈140–200 pm·rad)
Vertical Emittance | ~28 pm·rad | <10 pm·rad (design target)
Momentum Compaction (αc) | ~8.9 × 10⁻⁴ | ~8 × 10⁻⁵
Natural Bunch Length | ~15 ps | ~5.5 ps
Energy Loss per Turn | ~1.02 MeV | ~1.09 MeV
Lattice Type | DBA (Double-Bend Achromat) | 6BA (Six-Bend Achromat)
Number of Beamlines | 13 operating | Up to ~26 ports (planned)
Brilliance / Coherence | High | Ultra-high (order-of-magnitude increase)